## Slide 1: PROCEDURE FOR MACHINE LEARNING PREDICTIONS

## Slide 2: Data analysis
Columns name for data - ['Ni', 'Al', 'Co', 'Fe', 'Cr', 'Δsₘᵢₓ', 'VEC', 'δ', 'Δχ', 'ΔHₘᵢₓ' ,'Ω', 'Tm', 'phase']
Phase = 0 denotes FCC
Phase = 1 denotes FCC+BCC
Phase = 2 denotes BCC

## Slide 3
Plotted pairplots, heatmaps between all features
Plotted parallel coordinate plot for all features and 7 parameters showing different phase
Plotted radarplot for Al with different parameters
Plotted radarplots for phase relation with element composition

## Slide 4
Hexbin plots for Al and Ni with 7 parameters
Kde plots for Al, Cr, Ni with 7 parameters showing different phase

## Slide 5: ML for phase predictions
Splitted data into train set and test set with test size = 0.2 (20%)
Random state = 42 applied to have a same particular train set, test set while running code for more than 1 time
Train set size = 10223 datapoints
Test set size = 2556 datapoints
Whole data size = 12779 datapoints

## Slide 6
Trained algorithms on train set along with optimum parameters calculated by gridsearchcv
Optimum parameters were also calculated on the same train set, test size and same random state
Applied random state = 42 while training some algorithms like random forest , decision tree to have exact same results on running code again
For ANN, KNN minmax scaler (range 0-1) applied on data for better performance of algorithm

## Slide 7
Calculated training and testing accuracy
Plotted confusion matrix and feature importance for each algorithm

## Slide 8
Carried Predictions for prediction data with the trained algorithms
Plotted confusion matrix and Calculated accuracy of predicted phase with actual phase from calphad and 1200 C
Plotted RADARPLOT for prediction data (phase relation with element composition)

## Slide 9: Data analysis with density
Plotted pairplot, parallel coordinate plots , heatmaps for all parameters along with density
Kde jointplot, hexbin plots for all parameters wrt density
Radarplot for density relation with different parameters

## Slide 10: ML for density predictions
Columns name for data - ['Ni', 'Al', 'Co', 'Fe', 'Cr', 'Δsₘᵢₓ', 'VEC', 'δ', 'Δχ', 'ΔHₘᵢₓ' ,'Ω', 'Tm', 'density']
Same train , test size selected for training algorithms (test size= 0.2) , random state =42

## Slide 11
Trained algorithms on train set along with optimum parameters calculated by gridsearchcv
Optimum parameters were also calculated on the same train set, test size and same random state
Applied random state = 42 while training some algorithms like random forest , decision tree, gradient boosting to have exact same results on running code again
For ANN minmax scaler (range 0-1) applied on data for better performance of algorithm

## Slide 12
Calculated training and testing accuracy/ r2_score, MSE and MAE
Plotted actual vs predicted density comparison plots and feature importance for each algorithm

## Slide 13
Carried Predictions for prediction data with the trained algorithms
Plotted actual vs predicted density plots and Calculated r2_score, MAE